## Slide 1: Stability of zinc oxide samples prepared with sol- gel method in supercritical water
Ayten ATEŞ
Cumhuriyet University, Engineering Faculty, Department of Chemical Engineering, Sivas, 58140, TURKEY
3rd International Colloquium Energy and Environmental Protection

## Slide 2: Zinc Oxide (ZnO)
a white crystalline oxide of zinc
Structure
Hexagonal, wurtzite crystal structure
Outstanding optical and electrical properties
Uses
Optoelectric transducers,
Chemical and gas sensors,
Photocatalyst etc.
Morphologies
wires, flowers, rods, tubes, sheets, ribbons, plates, dumbbell, disks and springs
Synthesis routes
Sol–gel method
Hydrothermal and solvothermal synthesis from ambient temperature and pressure up to supercritical conditions
Chemical vapor deposition (CVD)
Thermal evaporation
Spray pyrolysis

## Slide 3: Use of supercritical water (SCW) with heterogeneous catalyst in biomass gasification has following advantages:
The control of phase behavior via elimination of gas- liquid and liquid- liquid mass transfer resistances,
Enhanced diffusion rate in reactions controlled by interface diffusion (fluid/particle),
Enhanced heat transfer,
Easy removal of products,
Improvement of catalyst’s lifetime by dissolution of deactivating hydrocarbons,
Improvement of solvent using a co-solvent and increased pressure.

## Slide 4: Effect of supercritical water (SCW) on heterogeneous catalyst
The stability and mechanical strength of the catalysts cannot be remained in SCW as the solid- solid transformations of the conventional catalysts.
The structural change such as the aggregation of solid catalysts, phase transformation and dissolution of solid can occur in SCW.
The degree of the structural change:
The composition of catalysts
Preparation method of catalysts
Operation conditions in the reactor.
The crystalline phase of zinc oxide strongly affects its structural, textural, and thereby catalytic properties in SCW

## Slide 5: Experimental Method
Sol-gel synthesis of ZnO
Precursor: Zinc acetate dehydrate
Chemical: Ethylene glycol, n-propyl alcohol, and glycerol, triethylene amine
Preperation: Precursor, zinc acetate dehydrate, was dissolved in ethylene glycol at 150 oC for 15 min at 400 rpm. The gel was formed during aging. The gel was dissolved in glycerol and n- propanol was added to solution. After gel formation, tri ethylene amine was added to the gel and the solvent was removed by rotary evaporator at 90 oC under vacuum. Gel was dried at 80 oC and calcined at 350 oC and 900 oC.
Characterization
Temperature-Programmed Reduction (TPR)
Temperature-Programmed Oxidation (TPO)
Crystalinity: XRD (Rigaku SmartLab).
Surface area and porosity (Autosorb 1)
Functional groups : FTIR (Perkin-Elmer Spectrum One)
Particle size: SEM / Particle size analyzer

## Slide 6
Reactor: Batch reactor (Parr 4591) (volume of 100 cm3).
Mixture: 55 g/L of formaldehyde and 40 g (0.52 g/cm3) of solution ;
ZnO catalyst: 1.0 g
Reaction time and temperature: 30 min and 400 oC
Gas and liquid samples were analyzed by using an on-line GC and HPLC, respectively
Reaction

## Slide 7
RESULTS AND DISCUSSION

## Slide 8
XRD
ZnO has hexagonal crystal structure and its crystal structure maintains after SCW gasification, but its crystal size is getting bigger based on SEM results

## Slide 9
SEM RESULTS
ZnO-350
ZnO-350SCW
ZnO-900
ZnO-900-SCW
ZnO calcined at 350 oC
has nano- sized particles
ZnO calcined at 900 oC
has mikro- sized particles
SCW gasification leads to
particle growing at both
calcination temperature

## Slide 10
SEM RESULTS
ZnO-350
ZnO-900
ZnO-350- HT
ZnO-900- HT
SCW leads to agglomeration of
ZnO irrespective of calcination temperature

## Slide 11: Surface area and pore size distribution
a Multipoint BET; b Adsorbed volume at P/Po = 0.99’da; c DR
Surface area of ZnO synthesized with sol- gel is higher than commercial ZnO
The reaction of formaldehyde on ZnO decreased surface area due to agglomeration of crystal
Sample | SBETa (m2g− 1) | VTotalb (cm3 g− 1) | Vmicro (cm3 g− 1) | Dp (Å) c
ZnO-Commercial | 9.7 | 0.04 | - | 167.0
ZnO-SJ-350 | 30.7 | 0.18 | 0.01 | 121.9
ZnO-SJ-350-HT | 21.5 | 0.16 | 0.006 | 151.0
ZnO-SJ-350-SCW | 11.65 | 0.10 | 0.003 | 176.8
ZnO-SJ-900 | 26.8 | 0.12 | - | 295
ZnO-SJ-900-HT | 20.5 | 0.06 | 0.006 | 54.1
ZnO-SJ-900-SCW | 9.94 | 0.10 | 0.003 | 203.1

## Slide 12
ZETA Results
SCW gasification and SCW affect significantly the zeta potential of ZnO
Hydrothermal treatment (HT) in SCW affects significantly the zeta potential
of ZnO

## Slide 13
TGA Results
ZnO calcined at high temperature (900 oC) is more stabile than that at low temperature
due to its higher crystal size based on SEM and XRD results
Coking is less in the presence of ZnO- 350 than that of ZnO-900
Coke amount

## Slide 14: Activity Results
Table 1. Gas and liquid product distribution of formaldehyde on ZnO
For 30 min, the highest H2 percentage is detected on ZnO-900 and highest CO2 percentage is observed on ZnO- 350. Increasing particle size increases hydrogen formation of ZnO.
Sample | mcat (g) | CH2O (%) | mTotal (g) | T (oC) | t (min) | CO2 | H2 | CO | O2 | CH4 | CCH2O (g/L) | CCH3OH (mol/L) | CHCOOH (mol/L) | %X | pH
Homogenous | - | 20 | 40 | 400 | 30 | 45.68 | 37.83 | 11.76 | 3.64 | 1.08 | 17.40 | 5.64 | 0.83 | 91.0 | 2.88
ZnO-350 | 1.0 | 20 | 40 | 400 | 30 | 43.24 | 53.84 | 1.80 | 0.65 | 0.42 | 14.90 | 3.58 | 0.74 | 92.6 | 2.45
ZnO-350-R | 1.0 | 20 | 40 | 400 | 30 | 41.54 | 54.68 | 1.48 | 1.85 | 0.39 | 3.10 | 5.81 | 0.22 | 98.4 | 3.01
ZnO-900 | 1.0 | 20 | 40 | 400 | 30 | 35.25 | 57.28 | 3.82 | 3.19 | 0.46 | 8.79 | 5.38 | 0.56 | 95.6 | 2.27
% 10 Formaldehyde-pH=3.20; % 15 Formaldehyde pH=2.58; % 20 Formaldehyde-pH=2.45 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 

## Slide 15: Decomposition mechanism of formaldehyde
The presence of ZnO changes decomposition mechanism of CH2O and enhanced hydrogen formation

## Slide 16: Results and Discussion
Based on XRD pattern:
ZnO has hexagonal phase composition irrespective of calcination temperature
SCW and SCW gasification do not affect ZnO’s phase composition
Increasing calcination temperature of ZnO :
increasing stability based on XRD patterns
decreasing surface area and porosity
increasing crystal size

## Slide 17
Presence of ZnO
changes decomposition mechanism of formaldehyde
enhances hydrogen formation
increases formaldehyde conversion

## Slide 18
THANKS
FINANCIAL SUPPORT The Scientific and Technological Research Council of Turkey (TUBITAK) (213 M398) and Cumhuriyet University Research Fund (M742).