## Slide 1: 3rd International Colloquium Energy and Environmental Protection 14 – 16 November 2018 Petroleum – Gas University of Ploiesti Romania
Removal of pollutants from wastewater resulted from biodiesel production by means of catalytic oxidation in suspension
Juganaru Traian (*)
Movileanu Daniela Luminita
Petroleum – Gas University of Ploiesti, Romania

## Slide 2
INTRODUCTION
glycerol is the main pollutant in wastewater resulted from biodiesel production plants
conversion of non- or hardly -biodegradable products in readily biodegradable products can be a solution for treatment of wastewater resulted from industrial chemical processes

## Slide 3
partial oxidation of glycerol in order to transform it into readily biodegradable products can be considered a posibility to reduce the pollution degree of wastewater from biodiesel plants, expressed as BOD5
this study presents the results obtained from partial catalytic oxidation in suspension of glycerol contained in a simulated wastewater

## Slide 4
Goals
GLYCEROL
catalyst
partial oxidation
readily biodegradable oxygenated products

## Slide 5
Possible products

## Slide 6: Laboratory plant
stirrer
condensation system
thermometer
reaction vessel
electrical water bath for heating
blowing air system

## Slide 7
simulated waste water preparation
1 % glycerol in water
usually, wastewater from biodiesel plants has  1% glycerol
BOD5 = 315 mg O2/L
Feedstock and Catalysts

## Slide 8
400 cm3 simulated waste water
3 g catalyst
air
a small amount of Ca(OH)2 in order to control the pH of reaction medium (pH = 8.5-9)
heating to 80-900C
6 h reaction time
1 sample/2h
samples cooling
catalyst filtration
BOD 5 analyse

## Slide 9
catalysts prepared by ICECHIM Bucharest
Manganese oxides nanoparticles
DLS analysis of manganese oxides : average size 260 nm

## Slide 10
Iron oxides nanoparticles
DLS analysis of iron oxides: average size 337.3 nm

## Slide 11: Results and conclusions
significant decrease of BOD5 with reaction time increase, for both catalyst systems (from 315 to 61 for Fe, respectively 35 mg O2/L for Mn)
higher decrease of BOD5 for manganese oxides catalyst use than iron oxides

## Slide 12
the highest decrease of BOD5 was recorded after first 2 hours of reacțion time, for both catalysts (96 mg O2/L for Fe and 125 mg O2/L for Mn)
after reaction time (6h), BOD5/Mn (35 mg O2/L) is nearly half than BOD5/Fe (61mg O2/L)
a significant difference between BOD5 values obtained for the two catalysts systems is registered after 4 hours reaction time  Fe-Mn = 41 mg O2/L

## Slide 13
extending the reaction time to 8 - 10 hours could lead to a BOD5 decrease in order to reach the maximum limits allowed by actual regulations
the difference between BOD5 values can be attributed either to the size of the catalysts’ nanoparticles (260 nm for Mn, respectively 337,3 nm for Fe) and/or to the metal nature

## Slide 14: THANK YOU FOR YOUR INTEREST!